LC928NB- Kitchen scale lower cost micro load cell

| Model: LC928NB Category: micro load cell Load range:3kg,5kg,7.5kg,10kg Dimension:26*26*1.0mm/1.5mm Material: alloy steel Application: handle scale, kitchen scale, micro force test equipment |
| --- |
| Specification |
| Comprehensive error: | 0.1%FS | Output resistance: | 500±10Ω |
| Rated output: | 0.75±0.15mv/v (3kg) 1.0±0.15mv/v (5-7.5kg) | Insulation resistance: | ≥2000MΩ(100VDC) |
| Non-linearity: | 0.05%FS | Excitation voltage: | 5~10VDC |
| Hysteresis: | 0.1%FS | Compensated temp: | -10~+40ºC |
| Repeatability: | 0.05%FS | Use temperature: | -20~+55ºC |
| Creep: | 0.1%FS/10Min | Temp effect on zero: | 0.05%FS/10ºC |
| Zero balance: | ±0.5mv | Temp effect on span: | 0.05%FS/10ºC |
| Input resistance: | 500±10Ω | Defend grade: | IP66 |